## Slide 1
Story Line
1. Background: To crystal structure analysis, we optimized the NaP₁₅ synthesis conditions and converted it into OP by MVLTG
2. Problem(obstacle): From EDX result Na-containing residues remain on OP crystal, pure crystal not yet synthesized
3. Key question: How to remove Na containing while synthesizing OP?
4. Speculation: Na removal is controlled by: NaP15 source size (shorter escaping channel) / DI water washing duration and cycles (eliminate blocks)/ post-heating (Provide Na escaping motivations)
5. Experimental design: NaP15 Ultrasonication → MVLTG(O2+Ar) → DI water washing → second MVLTG (O2+Ar) → DI water washing → mild heating with Ar
6. Characterization: Raman / HRTEM
7. Goal: High-purity OP samples for future γ-OP structural characterization
Synthesis and characterization of high-quality Orange Phosphorus
Title: